## Slide 1
Meeting with Thia on 9/3/19
Thia’s note from 9/3 meeting:
By end of September, expect to have:
– Two to three additional cells plus one sphere filled
– at least one new acceptable cell
– the sphere tested for RF cleaning
– further characterization of the existing cells
What was done in the month of September:
– Tommy filled at W&M, almost fully characterized – first good cell filled at W&M this time!
– Zhou filled at W&M, not yet tested
– sphere not done yet because we tried other new aspects in the filling procedure, still would like to try the sphere but at a later time.
– carefully studied Savior JLab data and found they are consistent with UVa latest data (JLab with vs. w/o convection and depending on whether heater tape is present, lifetime varies from 12 to 28 hours. UVa measured 14 hours with convection.).

## Slide 2
Plan for October
– Continue testing Tommy with higher AFP loss → more reliable in-beam estimate
– Plan to test Zhou at UVa this weekend (10/5-6)
– Mike now has a good inventory of windows
– Mike will make a new cell and ship to UVa this week, will take 1-2 weeks to fill.
– Mike will continue producing two to three more cells this month. These cells will be filled at UVa or W&M.
Jianping asked to bring good cells to JLab for pressure and density measurement.

## Slide 3
Current Target Cell Status for A1n/d2n
Cell name | fill date | cold spin down lifetime (hrs) | Max polarization | Expected in-beam polarization | Current status
Dutch | 8/22/2019 | 29.4 (UVa) | 54% (UVa) | 53% | at UVa
Fulla | 9/7/2018 | 17 (UVa); 15 (JLab) | 53% (UVa); 54% (JLab) | 50% | boxed up at JLab
TOMMY | 9/11/2019 | 15.2 (UVa) | 54% (UVa) | 49% | potentially a good cell but need careful AFP loss analysis
Brianna | 3/27/2019 | 23 (UVa before damage) | 53% (UVa before damage) | 48% (before damage) | laser damage, may retest
Savior | 10/27/2016 | 42 (UVa, 2016); 12-28 (JLab); 14.3 (UVa 2019 w convection) | 65% (UVa); 38% (JLab); 40% (UVa 2019) | 60% (2016) →?? | laser damage, not a good backup cell
Flurence | 9/28/2018 | 11 (UVa) | 45% (UVa) | 44% | backup cell
Other cells made before July 24, 2019 meeting: Noah (3/07), Elle (3/29), Sandy-II (5/28), Phoenix (6/3);
Other cells made after July 24, 2019 meeting: Zoe, Yeti (broke), Wayne;
New cell Zhou filled on 9/27/2019, not tested yet